| Date | Yb(OTf)3 g molL-1x102 | IB g molL-1 | Salt Mixture g/g/g mL | Emulsifier g |
| --- | --- | --- | --- | --- |
| 11/22/00 | 5 36.6 | 5 4.06 | 9H2O/4.5CaCl2/2.5MgCl2 17 | 0.1 DTAB |
| 11/22/00 | 1 36.6 | 1 4.06 | 1.8H2O/0.9CaCl2/0.5MgCl2 3.4 | 0.02 DTAB |
| 12/8/00 | 5 36.6 | 5 4.06 | 9H2O/4.5CaCl2/2.5MgCl2 17 | 0.1 DTAB |
| 12/8/00 | 1 36.6 | 1 4.06 | 1.8H2O/0.9CaCl2/0.5MgCl2 3.4 | 0.02 DTAB |
| 12/20/00 | 1 36.6 | 1 4.06 | 1.8H2O/0.9CaCl2/0.5MgCl2 3.4 | 0.02 DTAB |
| 1/06/01 | 0.5 4.03 | 10 8.93 | none | none |
| 1/06/01 | 0.5 4.03 | 10 8.93 | none | none |
| 1/06/01 | 0.5 1.99 | 10 4.41 | 0.5 H2O 0.5 | none |

| 1/06/01 | 0.5 1.99 | 10 4.41 | 0.5 H2O 0.5 | none |
| --- | --- | --- | --- | --- |
| 1/10/01 | 0.5 5.37 | 5 5.95 | none | none |
| 1/10/01 | 0.5 5.37 | 5 5.95 | none | none |
| 1/22/01 | 0.5 4.03 | 10 8.93 | 0.5 H2O 0.5 | none |
| 1/24/01 | 0.5 4.03 | 10 8.93 | 0.5 H20 0.5 | none |
| 1/24/01 | 0.5 5.37 | 5 5.95 | none | 0.1 DTAB |
| 1/24/01 | 1 17.2 | 1 1.90 | 1.8H2O/0.9CaCl2/0.5MgCl2 17 | 0.1 DTAB |
| 2/13/01 | 5 36.6 | 5 4.06 | 9H2O/4.5CaCl2/2.5MgCl2 17 | 0.1 DTAB |
| 2/13/01 | 5 36.6 | 5 4.06 | 9H2O/4.5CaCl2/2.5MgCl2 17 | 0.1 DTAB |

| 2/22/01 | 5 29.8,25.2,21.8,19.2 | 5 3.31,5.58,7.24,8.50 | 9H2O/4.5CaCl2/2.5MgCl2 17 | 0.1 DTAB |
| --- | --- | --- | --- | --- |
| 3/3/01 | 5 36.6,29.8,25.2,21.8 | 5 4.06,6.61,8.37,9.65 | 9H2O/4.5CaCl2/2.5MgCl2 17 | 0.1 DTAB |
| 3/6/01 | 5 36.6,29.8,25.2,21.8 10.5 | 5 4.06,6.61,8.37,9.65, 13.9 | 9H2O/4.5CaCl2/2.5MgCl2 17 | 0.1 DTAB |
| 3/9/01 | 5 36.6,29.8,25.2,21.8 10.5 | 5 4.06,6.61,8.37,9.65, 13.9 | 9H2O/4.5CaCl2/2.5MgCl2 17 | 0.1 DTAB |
| 3/16/01 | 1 5.37 | 5 2.98 | 19.2H2O/5.9LiCl/0.9MgCl2 25 | 0.2 DTAB |
| 3/16/01 | 1 5.37 | 5 2.98 | 19.95H2O/5.75LiCl/0.3NaCl 25 | 0.2 DTAB |
| 3/21/01 | 5 20.2 | 10 4.46 | 26.84H2O/7.08LiCl/1.08MgCl2 30 | 0.1 DTAB |
| 4/2/01 | 5 20.2 | 10 4.46 | 26.84H2O/7.08LiCl/1.08MgCl2 30 | 0.1 DTAB |
| 4/10/01 | 1 4.03 | 10 4.46 | 26.84H2O/7.08LiCl/1.08MgCl2 30 | 0.1g Betaine |

| 4/12/01 | 1 5.37 | 10 5.95 | 16.16H2O/4.6LiCl/0.24MgCl2 20 | 0.1 DTAB |
| --- | --- | --- | --- | --- |
| 4/12/01 | 1 5.37 | 10 5.95 | 16.16H2O/4.6LiCl/0.24MgCl2 20 | 0.1 DTAB |
| 4/18/01 | 1 4.03 | 10 4.46 | 16.16H2O/4.6LiCl/0.24MgCl2 20 | 0.1 hexdecyltrimethyl phosphonium Br |
| 4/18/01 | 1 4.03 | 10 4.46 | 16.16H2O/4.6LiCl/0.24MgCl2 20 | 0.1 hexdecyltrimethyl phosphonium |
| 4/18/01 | 1 4.03 | 10 4.46 | 16.16H2O/4.6LiCl/0.24MgCl2 20 | 0.1 hexdecyltrimethyl phosphonium |
| 4/19/01 | 1 5.04 | 10 5.58 | 18.16H2O/4.6LiCl/1.24MgCl2 22 | 0.1 DTAB |
| 4/19/01 | 1 5.04 | 10 5.58 | 18.16H2O/4.6LiCl/1.24MgCl2 22 | 0.1 DTAB |
| 4/19/01 | 1 8.06 | 10 8.93 | none | none |
| 4/20/01 | 1 8.06 | 10 8.93 | none | none |

| 4/20/01 | 1 4.88 | 10 5.41 | 16.16H2O/4.6LiCl/0.24MgCl2 20 | THF |
| --- | --- | --- | --- | --- |
| 4/20/01 | 1 5.20 | 10 5.76 | 16.16H2O/4.6LiCl/0.24MgCl2 20 | THF |
| 4/20/01 | 1 6.20 | 10 6.87 | 10.92H2O/3.54LiCl/0.54MgCl2 15 | THF |
| 4/22/01 | 1 8.06 | 10 8.93 | none | none |
| 4/23/01 | 1 8.06 | 10 8.93 | none | none |

| Solvent g molL-1 | Additives g molL-1 | Time hr | Temperature (C | Polymer %Conv./Mn/PDI |
| --- | --- | --- | --- | --- |
| none | 0.04 DtBP 9.5x10-3 | 7 | -58 | none |
| none | 0.9 DtBP 1.08 | 7 | -58 | none |
| none | 0.04 DtBP 9.5x10-3 | 7 | -58 | 12/3255/1.12 * |
| none | 0.9 DtBP 1.08 | 7 | -58 | 10/3265/1.12 * |
| none | none | 12 | -35 | none |
| 10 THF 6.93 | none | 4 | -78 | none |
| 10 THF 6.93 | none | 4 | -35 | none |
| 30 THF 9.24 | none | 4 | -78 | none |

| 30 THF 9.24 | none | 4 | -35 | none |
| --- | --- | --- | --- | --- |
| 5 THF/5 CH3NO2 4.62/5.46 | none | 4 | -78 | none |
| 5 THF/5 CH3NO2 4.62/5.46 | none | 4 | -35 | none |
| 9.5 EtOH 10.3 | none | 6 | -57 | none |
| 9.5 EtOH 10.3 | none | 6 | -35 | none |
| 10 EtOH 14.3 | none | 6 | -35 | none |
| 5 EtOH 4.72 | none | 6 | -35 | none |
| none | 0.25 cumyl-OH 8.42x10-2 | 12 | -35 | none |
| none | 0.25 tBu-OH 1.53x10-1 | 12 | -35 | none |

| 5 hexane 2.15 | none | 2,4,6,8 | -55 | Yes-see 1st IMA * |
| --- | --- | --- | --- | --- |
| none | none | 2,4,6,8 | -55 | No- froze |
| none | none | 2,4,6,8,24 | -55 | 2.7/288/1.8 ** 12.7/848/1.12 4.38/16.4k/1.87 |
| none | none | 2,4,6,8,24 | -55 | none |
| none | none | 8 | -57 | none |
| none | none | 8 | -57 | none |
| none | none | 8 | -57 | none |
| none | none | 8 | -60 | none |
| none | 0.22 cumyl-Cl 3.57x10-2 | 8 | -35 | none |

| none | 0.238 HCl 9.60x10-2 | 24 | -35 | none |
| --- | --- | --- | --- | --- |
| none | 0.22 cumyl-Cl 4.76x10-2 | 24 | -35 | none |
| 10 hexane 2.91 | 0.1 HSO3CF3 1.66x10-2 | 24 | -35 | <2% total low MW 186/1.10 high MW 864/1.04 |
| 10 hexane 2.91 | 0.22 cumyl-Cl 3.57x10-2 | 24 | -35 | <2%/903/1.04 |
| 10 hexane 2.91 | none | 24 | -35 | <2%/888/1.04 |
| none | 0.22 cumyl-Cl 4.46x10-2 | 24 | -35 | <2% total GPC in progress |
| none | none | 24 | -35 | <2% total GPC in progress |
| 10 THF 6.93 | 0.22 cumyl-Cl 7.14x10-2 | 24 | -35 | Between 60-80% 36,800/1.32 |
| 10 THF 6.93 | 0.22 cumyl-Cl/0.1 DtBP 2.61x10-2/7.14x10-2 | 24 | -35 | none |

| 3 THF 1.26 | 0.22 cumyl-Cl 4.33x10-2 | 24 | -50 | <2% total GPC in progress |
| --- | --- | --- | --- | --- |
| 1 THF 4.47x10-1 | 0.22 cumyl-Cl 4.61x10-2 | 24 | -50 | <2% total GPC in progress |
| 1 THF 5.33x10-1 | 0.22 cumyl-Cl 5.49x10-2 | 24 | -50 | <2% total GPC in progress |
| 10 THF 6.93 | 0.22 cumyl-Cl 7.14x10-2 | 24 | -35 | Yes, between 70-80% Appears to be poly THF GPC in progress |
| 10 MeOH 15.6 | 0.22 cumyl-Cl 7.14x10-2 | 24 | -35 | none |
|  | * Indicates that the reaction was either preformed by Stas or that the polymerization mixture was provided by Stas. ** Polymerization mixture prepared by Stas. Only reactions at 2,6,24 hr yielded polymer. The final sample had the appearance of low MW PIB, yet GPC shows a crude peak in the high MW region. DTAB stands for dodecyltrimethylammonium bromide Most reactions were thermally quenched with H2O. THF/H2O was used only for IMA reactions. |